For Official Use Only

GOVERNMENT OF INDIA

HKKJR  LJDKJ

MINISTRY OF RAILWAYS

JSY	EA=KY;

Consultancy Report

ON

Construction of high Bank in Between Vinaiki-Sikara Stations, Jabalpur-Gondia Gauge

Conversion Line in Nagpur Division, South East Central Railway

Consultancy No. RDSO/2010/GE:CR-0142

May - 2010

Geo-technical Engineering Directorate

HKW&RDUHDH BATHFU;JH FUNS’KKY;

Research Designs & Standards Organisation

VUQLA/KKU VFHKDYI VKSJ EKUD LAXBU

Lucknow – 226011

Y[KUÅ & 226011

1

INDEX

| SL | Contents | Page |
| --- | --- | --- |
|  | Preface | 2 |
|  | Synopsis | 3 |
| 1. | Introduction | 4 |
| 2. | Reference | 4 |
| 3. | Details of soil samples | 4 |
| 4. | Slope Stability analysis with Slope/W software | 4 |
| 5. | Summary Of Test Results | 6 |
| 6. | Recommendations | 7 |
| 1-5 | Annexures | 10-14 |
|  | Recommended Profile |  |

1

PREFACE

This report is prepared on the basis of soil investigation & soil samples collected by railway and submitted to RDSO; vide Dy. Chief Engineer (con), South East Central railway, Jabalpur letter no. Nil, dated 22.10.2009. And soil sample tested in Geo-technical Engineering lab of RDSO. Views expressed are subject to modification from time to time in the light of future developments on the subject and as such, do not represent the views of Ministry of Railways (Railway Board), Government of India.

This report is the property of the RDSO and is meant essentially for officials use. It may not be loaned, reproduced in part or in full or quoted as an authority without the permission of Director General, RDSO.

(Rajesh Agarwal) Director/ Geotech. Engg

(J.C. Parihar)

Sr. Executive Director/Geotech. Engg.

2

SYNOPSIS

New alignment between Vinaiki-Sikara stations, Jabalpur-Gondia Gauge Conversion Project, Nagpur division, South East Central Railway is under construction in which high embankment locations as high as 25.0 M exist. Dy. Chief Engineer (Con) South East Central railway requested for slope design of high bank in the section for construction of Jabalpur-Gondia Gauge Conversion Line, Nagpur Division, South East Central Railway. For this purpose he arranges to collect soil samples and sent to RDSO.

Present report includes embankment profile suitable for construction, based on soil samples collected by railway and sent to RDSO; vide Dy. Chief Engineer (con), South East Central railway, Jabalpur letter no. Nil, dated 22.10.2009, and soil sample tested in Geo-technical Engineering lab of RDSO. Recommendations include embankment profile and provision of suitable thickness of blanket material & protection of embankment slope by dry stone pitching/retaining walls etc.

3

1.0	Introduction

In Jabalpur-Gondia Gauge Conversion line (diversion portion) it is requred to construct 25.0 meters height embankment between Vinaiki-Sikara stations at Chanage 7700 to 9200. The height of bank at many locations is more than 6.0 m and some locations height of bank as 25.0 m also.

2.0	Reference

Dy. Chief Engineer referred these problems to RDSO vide his letter No. Nill, dated 22.10.2009 and requested for slope design of high embankment in the section.

3.0	Details of soil samples

The soil samples were tested in Geo-technical Engineering Laboratory of RDSO for following tests:

- Natural Moisture Content (NMC)

- Natural Dry Density (NDD)

- Optimum moisture content (OMC)

- Maximum Dry Density (MDD)

- Grain Size analysis

- Consistency Limits

- Specific Gravity

- Triaxial shear test in Consolidated Undrained condition with measurement of pore pressure (CU)

4.0	Slope Stability analysis with Slope/W software

Slope stability analysis has been carried out with the help of ‘SLOPE/W’ software by taking the results of soil samples collected by railway and sent to RDSO; vide Dy. Chief Engineer (con), South East Central railway, Jabalpur letter no. Nil, dated 22.10.2009. And soil sample tested in Geo-technical Engineering lab of RDSO. SLOPE/W is a software that uses the limit equilibrium theory for finding out the factor of safety of earth and rock slopes. The inbuilt verstabty comprehensive formation of SLOPE/W makes it possible to select a variety of methods for computing the factor of safety and to analyses both simple and complex geometric pattern and loading conditions. However, the limitations of SLOPE/W software are as follows:-

- Details calculations of slope stability analysis are not shown by SLOPE/W software.

4

- This software analyses only two-dimensional problems.

With the help of SLOPE/W software, all the locations desired by the railway have been analysised to achieve factor of safety minimum 1.4 envisaged by the “Guidelines for earthwork in railway project Guideline No. GE:G-1 July 2003”. Analysis and designed profile are placed at Annexure 1-5.

5

5.0	Summary Of Test Results

Test results of samples from Ch.7700 to Ch.9200 are tabulated below:

|  |  | Embankment Soil (Fill material) |  |  |  |  |  |  | Sub-Soil (Alignment soil) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Tests Name |  |  | Ch.7990 |  | Ch.8350 | Ch.8450 | Ch.8650 | Ch.8000 | Ch.8250 |  | Ch.8600 | Ch.8700 | Ch.8900 |
| Soil Sample D*/UD* |  |  | D |  | D | D | D | UD | UD |  | UD | D | UD |
| Soil Classification |  |  | GM |  | SM | SW-SM | SM | SM | SM |  | SW-SM | SM | SM |
| Natural Moisture |  | Content | - |  | - | - | - | 29.88 | 20.56 |  | 15.89 | - | 19.16 |
| (NMC)% |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Natural Dry density gm/cc |  |  | - |  | - | - | - | 1.331 | 1.631 |  | 1.056 | - | 1.349 |
| Gravel (%) |  |  | 54 |  | 08 | 08 | 22 | 03 | 12 |  | 23 | 20 | 16 |
| Sand (%) |  |  | 31 |  | 70 | 83 | 64 | 48 | 55 |  | 66 | 58 | 36 |
| Silt (%) |  |  | 14 |  | 22 | 09 | 14 | 48 | 30 |  | 11 | 22 | 44 |
| Clay (%) |  |  | 00 |  | 00 | 00 | 00 | 01 | 03 |  | 00 | 00 | 04 |
| Passing 75 | micron sieve |  | 14 |  | 22 | 09 | 14 | 49 | 33 |  | 11 | 22 | 48 |
| (%) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Optimum Moisture content |  |  | 12.80 |  | 9.20 | 9.60 | 10.00 | - | - |  | - | 11.00 | - |
| (%) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Maximum | Dry | Density | 1.893 |  | 1.720 | 1.890 | 1.884 | - | - |  | - | 1.872 | - |
| gm/cc |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Specific Gravity |  |  | 2.49 |  | 2.25 | 2.36 | 2.04 | 2.54 | 2.43 |  | 2.43 | 2.30 | 2.34 |
| Consistency Limits |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Liquid Limit (LL) % |  |  | NP |  | NP | NP | NP | 46 | 40 |  | 49 | NP | 60 |
| Plastic Limit (PL) % |  |  | NP |  | NP | NP | NP | 28 | 27 |  | 33 | NP | 34 |
| Plasticity Index |  |  | NP |  | NP | NP | NP | 18 | 13 |  | 16 | NP | 26 |
| Shear Parameters (CU) test Triaxial |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Cohesion (Cʹ) kg/cm² |  |  | 0.01 |  | 0.006 | 0.000 | 0.006 | 0.044 | 0.034 |  | 0.022 | 0.007 | 0.050 |
| Angle of Internal |  | Friction | 35.04 |  | 33.22 | 34.25 | 33.77 | 30.32 | 31.39 |  | 35.09 | 33.01 | 31.94 |
| (ϕʹ) degree |  |  |  |  |  |  |  |  |  |  |  |  |  |

*D : Disturbed Soil Sample

*UD : Un-Disturbed Soil Sample

6

6.0	Recommendations

Slope Stability analysis has been analysed for embankment as per soil samples collected by railway and sent to RDSO; vide Dy. Chief Engineer (con), South East Central railway, Jabalpur letter no. Nil, dated 22.10.2009. And soil sample tested in Geo-technical Engineering lab of RDSO. Following recommendations are made:

- At Ch. 8000, embankment height is 18.246 m (As per CE/C/BSP’s DRG No.5190/08). Considering embankment height for slope design 19.0 m, suggested profile of embankment slope is 2.5:1 along with 3.0 m berm at every 6.0 m height (Annexure-1). The fill material for this

location should be taken from Ch.7990, whose soil properties are as classification GM, Cʹ =0.01 kg/cm², ϕʹ=35.040 and MDD= 1.893 g/cm².

- At Ch. 8250, embankment height is 25.577 m (As per CE/C/BSP’s DRG

No.5190/08). Considering embankment height for slope design 26.0 m, suggested of embankment slope 2.75:1 with 3.0 m berm at every 6.0 m height (Annexure-2). The fill material for this location should be taken from Ch.8350, whose soil properties are as; soil classification SM, Cʹ =0.006 kg/cm², ϕʹ=33.220 and MDD= 1.72 g/cm².

- At Ch. 8600, embankment height is 20.630 m (As per CE/C/BSP’s DRG No.5190/08). Considering embankment height for slope design 21.0 m, suggested profile of embankment slope 2.75:1 with 3.0 m berm at every 6.0 m height (Annexure-3). The fill material for this location

should be taken from Ch.8650, whose soil properties are as; soil classification SM, Cʹ =0.006 kg/cm², ϕʹ=33.770 and MDD= 1.884 g/cm².

- At Ch. 8700, embankment height is 20.432 m (As per CE/C/BSP’s DRG No.5190/08). Considering embankment height for slope design 21.0 m, suggested profile of embankment slope 2.75:1 with 3.0 m berm at every 6.0 m height (Annexure-4). The fill material for this location

should be taken from Ch.8650, whose soil properties are as; soil classification SM, Cʹ =0.006 kg/cm², ϕʹ=33.770 and MDD= 1.884 g/cm².

- At Ch. 8900, embankment height is 14.573 m (As per CE/C/BSP’s DRG No.5190/08). Considering embankment height for slope design 15.0 m, suggested profile of embankment slope 2.75:1 with 3.0 m berm at every 6.0 M height (Annexure-5). The fill material for this location

should be taken from Ch.8650, whose soil properties are as; soil classification SM, Cʹ =0.006 kg/cm², ϕʹ=33.770 and MDD= 1.884 g/cm².

Above details are scrutinized in the following table:

| S. | Locations | Height of | Recommended slope& | Reference |
| --- | --- | --- | --- | --- |
| N. |  | embankment | berm width | Annexure |
| 1. | Ch.8000 | 19 m | 2.5:1 & 3.0 m | 1 |
| 2. | Ch. 8250 | 26 m | 2.75:1 & 3.0 m | 2 |
| 3. | Ch. 8600 | 21 m | 2.75:1 & 3.0 m | 3 |
| 4. | Ch.8700 | 21 m | 2.75:1 & 3.0 m | 4 |
| 5. | Ch. 8900 | 15 m | 2.75:1 & 3.0 m | 5 |

6.2	General Points

- For protection of embankment slope dry stone pitching 60 cm above HFL is recommended to protect erosion of slope of the embankment due to flow of water.

- Erosion control measures like turfing should be carried out.

- Depth of blanket layer depends primarily on the type of sub-grade soil and axle load of the traffic. For blanket thickness provision in the para 4.3.2 of “Guidelines for earthwork in railway project Guideline No. GE:G-1 July 2003” should be adopted. Alternatively depth of blanket can be decided from the provisions of the recent approved ‘Guidelines & Specifications of Formation Design for Heavy Axle Load, Report No.2007/GE:G-0014, November-2009.

8

Officers And Staff Associated with Preparation Of report

The report has been prepared by Shri Rajesh Agarwal, Director/Geotechnical Engineering under guidance of Shri J.C. Parihar, Sr. Executive Director/Geotechnical Engineering.

This report has been prepared on the basis of soil samples collected by railway and sent to RDSO. And soil sample tested in Geo-technical Engineering lab of RDSO. The following officer and staff of Geotechnical engineering directorate were associated with the preparation of report.

- Shri S.K. Awasthi, ARE

- Shri Samay Singh, SRE

- Shri Sandeep Kumar, SRE

The following staffs were associated with soil testing:

- Shri Shiv Kumar, SSRE

- Shri Nirbhay Kumar Singh, SRE

- Shri D.K. Srivastav,SRE

- Shri S.D. Sharma, JRE-1

- Shri B.K. Das, JRE-1

9

Annexure – 1

Elevation (m)

Jabalpur-Gondia GC Project

Chainage 8000

Height 19.0 m

Slope 2.5:1

Berm 3.0

FOS 1.469

| 89 |  |  |
| --- | --- | --- |
| 86 |  |  |
| 83 |  |  |
| 80 |  |  |
| 77 | Slope 2.5:1 |  |
| 74 | Berm 3 m |  |
| 71 | Slope 2.5:1 |  |
| 68 |  |  |
|  |  | Berm 3 m |
| 65 | Embankment Soil | Slope 2.5:1 |
| 62 |  | Berm 3 m |
| 59 |  | Slope 2.5:1 |
| 56 |  |  |
| 53 |  |  |
| 50 |  | Sub Soil |
| 47 |  |  |
| 44 |  |  |
| 41 |  |  |
| 38 |  | Bedrock |
| 35 |  |  |
| 32 |  |  |

Soil1

Embankment Soil

SoilModelMohr-Coulomb

Unit Weight 21.1

Cohesion 1

Phi35.04

Unsaturated PhiB 0

Piezometric Line # 0

Ru (added) 0.25

Pore-Air Pressure 0

Soil2

Sub Soil

SoilModelMohr-Coulomb

Unit Weight 18.1

Cohesion 4.4

Phi30.32

Unsaturated PhiB 0

Piezometric Line # 0

Ru (added) 0.25

Pore-Air Pressure 0

Soil3

Bedrock

SoilModelBedrock

Unit Weight -1

Piezometric Line # 0

Ru (added) 0

Pore-Air Pressure 0

12 16 20 24 28 32 36 40 44 48 52 56 60 64 68 72 76 80 84 88 92 96 100 104 108 112 116 120 124 128 132 136 140 144 148 152

HorizontalDistance (m)

10

Annexure – 2

Jabalpur-Gondia GC Project

Chainage 8250

Height 26.0 m

Slope 2.75:1

Berm 3.0

FOS 1.447

|  | 84 |  |  |
| --- | --- | --- | --- |
|  | 81 |  |  |
|  | 78 | Slope 2.75:1 |  |
|  | 75 |  |  |
|  |  | Berm 3 m |  |
|  | 72 |  |  |
|  |  | Slope 2.75:1 |  |
|  | 69 |  |  |
|  |  |  | Berm 3 m |
|  | 66 |  |  |
|  | 63 |  | Slope 2.75:1 |
|  |  | Embankment Soil | Berm 3 m |
|  | 60 |  |  |
|  | 57 |  | Slope 2.75:1 |
|  |  |  | Berm 3 m |
|  | 54 |  |  |
|  |  |  | Slope 2.75:1 |
|  | 51 |  |  |
|  | 48 |  |  |
| (m) | 45 |  |  |
|  | 42 |  |  |
| Elevation | 39 |  |  |
|  | 27 |  | Sub Soil |
|  | 36 |  |  |
|  | 33 |  |  |
|  | 30 |  |  |
|  | 24 |  |  |
|  | 21 |  |  |
|  | 18 |  |  |
|  | 15 |  |  |

Soil1

Embankment Soil

SoilModelMohr-Coulomb

Unit Weight 19.4

Cohesion 0.6

Phi33.22

Unsaturated PhiB 0

Piezometric Line # 0

Ru(added) 0.25

Pore-Air Pressure 0

Soil2

Sub Soil

SoilModelMohr-Coulomb

Unit Weight 19.6

Cohesion 3.4

Phi31.39

Unsaturated PhiB 0

Piezometric Line # 0

Ru (added) 0.25

Pore-Air Pressure 0

Soil3

Bedrock

SoilModelBedrock

Unit Weight -1

Piezometric Line # 0

Ru (added) 0

Pore-Air Pressure 0

15 19 23 27 31 35 39 43 47 51 55 59 63 67 71 75 79 83 87 91 95 99103 109 115 121 127 133 139 145 151 157 163 169 175

HorizontalDistance (m)

11

Annexure – 3

Elevation (m)

| Jabalpur-Gondia GC Project |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Soil1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Embankment Soil |
| Chainage 8600 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | SoilModelMohr-Coulomb |
| Height 21.0 m |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | UnitWeight 19.6 |
| Slope 2.75:1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Cohesion 0.6 |
| Berm | 3.0 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Phi33.77 |
| FOS 1.491 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Unsaturated PhiB 0 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Piezometric Line # 0 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Ru (added) 0.25 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Pore-Air Pressure 0 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Soil2 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Sub Soil |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | SoilModelMohr-Coulomb |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | UnitWeight 16.22 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Cohesion 2.2 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Phi35.09 |
| 79 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Unsaturated PhiB 0 |
| 76 |  |  |  | Slope 2.75:1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Piezometric Line # 0 |
| 73 |  |  |  |  |  |  | Berm 3 m |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Ru (added) 0.25 |
| 70 |  |  |  |  |  |  |  |  | Slope 2.75:1 |  |  |  |  |  |  |  |  |  |  |  |  | Pore-Air Pressure 0 |
| 67 |  |  |  |  |  |  |  |  |  |  |  | Berm 3 m |  |  |  |  |  |  |  |  |  | Soil3 |
| 64 |  |  |  | Embankment Soil |  |  |  |  |  |  |  |  | Slope 2.75:1 |  |  |  |  | 3 m |  |  |  |  |
| 61 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Berm |  |  |  |  |  | Bedrock |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Slope 2.75:1 |  |  |  | SoilModelBedrock |
| 58 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | UnitWeight -1 |
| 55 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Piezometric Line # 0 |
| 52 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Ru (added) 0 |
| 49 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Pore-Air Pressure 0 |
| 46 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 43 |  |  |  |  |  |  |  |  |  |  |  |  | Sub Soil |  |  |  |  |  |  |  |  |  |
| 40 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 37 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 34 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 31 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 28 |  |  |  |  |  |  |  |  |  |  |  |  |  | Bedrock |  |  |  |  |  |  |  |  |
| 25 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 22 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 12 | 16 | 20 | 24 | 28 | 32 | 36 | 40 | 44 | 48 | 52 | 56 | 60 | 64 | 68 | 72 | 76 | 80 | 84 | 88 | 92 | 96 100 104 108 112 116 120 124 128 132 136 140 144 148 152 |  |

HorizontalDistance (m)

12

Annexure – 4

Elevation (m)

|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Soil1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Jabalpur-Gondia GC Project |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Embankment Soil |
| Chainage 8700 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | SoilModelMohr-Coulomb |
| Height 21.0 m |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Unit Weight 19.6 |
| Slope 2.75:1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Cohesion 0.6 |
| Berm | 3.0 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Phi33.77 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Unsaturated PhiB 0 |
| FOS 1.491 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Piezometric Line # 0 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Ru (added) 0.25 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Pore-Air Pressure 0 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Soil2 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Sub Soil |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | SoilModelMohr-Coulomb |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Unit Weight 20.6 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Cohesion 0.7 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Phi33.01 |
| 79 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Unsaturated PhiB 0 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Piezometric Line # 0 |
| 76 |  |  |  | Slope 2.75:1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Ru (added) 0.25 |
| 73 |  |  |  |  |  |  | Berm 3 m |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Pore-Air Pressure 0 |
| 70 |  |  |  |  |  |  |  |  | Slope 2.75:1 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 67 |  |  |  |  |  |  |  |  |  |  |  | Berm 3 m |  |  |  |  |  |  |  |  |  | Soil3 |
|  |  |  |  | Embankment Soil |  |  |  |  |  |  |  |  | Slope 2.75:1 |  |  |  |  |  |  |  |  |  |
| 64 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Bedrock |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Berm 3 m |  |  |  |  |  |  |
| 61 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | SoilModelBedrock |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Slope 2.75:1 |  |  |  |  |
| 58 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Unit Weight -1 |
| 55 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Piezometric Line # 0 |
| 52 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Ru (added) 0 |
| 49 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Pore-Air Pressure 0 |
| 46 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 43 |  |  |  |  |  |  |  |  |  |  |  |  | Sub Soil |  |  |  |  |  |  |  |  |  |
| 40 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 37 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 34 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 31 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 28 |  |  |  |  |  |  |  |  |  |  |  |  |  | Bedrock |  |  |  |  |  |  |  |  |
| 25 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 22 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 12 | 16 | 20 | 24 | 28 | 32 | 36 | 40 | 44 | 48 | 52 | 56 | 60 | 64 | 68 | 72 | 76 | 80 | 84 | 88 | 92 | 96 100 104 108 112 116 120 124 128 132 136 140 144 148 152 |  |

HorizontalDistance (m)

13

Annexure – 5

Elevation (m)

Jabalpur-Gondia GC Project

Chainage 8900

Height 15.0 m

Slope 2.75:1

Berm 3.0

FOS 1.489

| 97 |  |  |
| --- | --- | --- |
| 94 |  |  |
| 91 |  |  |
| 88 |  |  |
| 85 |  |  |
| 82 |  |  |
| 79 |  |  |
| 76 | Slope 2.75:1 |  |
| 73 | Berm 3 m |  |
| 70 | Slope 2.75:1 |  |
| 67 | Embankment Soil | Berm 3 m |
| 64 |  | Slope 2.75:1 |
| 61 |  |  |
| 58 | Sub Soil |  |
| 55 |  |  |
| 52 |  |  |
| 49 | Bedrock |  |
| 46 |  |  |
| 43 |  |  |
| 40 |  |  |

Soil1

Embankment Soil

SoilModelMohr-Coulomb

Unit Weight 19.6

Cohesion 0.6

Phi33.77

Unsaturated PhiB 0

Piezometric Line # 0

Ru (added) 0.25

Pore-Air Pressure 0

Soil2

Sub Soil

SoilModelMohr-Coulomb

Unit Weight 17.73

Cohesion 5

Phi31.94

Unsaturated PhiB 0

Piezometric Line # 0

Ru (added) 0.25

Pore-Air Pressure 0

Soil3

Bedrock

SoilModelBedrock

Unit Weight -1

Piezometric Line # 0

Ru (added) 0

Pore-Air Pressure 0

12 16 20 24 28 32 36 40 44 48 52 56 60 64 68 72 76 80 84 88 92 96 100 104 108 112 116 120 124 128 132 136 140 144 148 152

HorizontalDistance (m)

14